## Slide 1
Tao Xiang
Institute of Physics
Chinese Academy of Sciences
txiang@iphy.ac.cn
High-Tc Superconductivity
by Metallizing Strong-bonding Electrons

## Slide 2
What is superconductor?
Heike Kamerlingh Onnes
Ideal Conductor: zero resistance
Walther Meissner
Ideal Diamagnet: Messiner Effect
Critical temperature

## Slide 3
High-Tc Superconductors Discovered
Cuprate SC
30~160 K
Iron-based SC
30~56 K
MgB2
39 K
H3S and other H-enriched SC
100~280K
Superconducting transition temperature ~ 40 K or higher
It is not difficult to find superconductors
But it is difficult to find high-Tc superconductors

## Slide 4
By PJRay, https://commons.wikimedia.org/w/index.php?curid=4619314
Timeline of Discovered Superconductors
cuprates
Fe-based

## Slide 5
How to become a superconductor?
Electrons must form Cooper pairs: any two electrons should form a bound state
Cooper pairs must condense to form phase coherence
Bardeen Cooper Schrieffer
1957 / 1972
Binding energy of Cooper pair
determines the transition temperature
Larger , higher

## Slide 6
Polarization of the lattice by one electron leads to an attractive potential for another electron, which binds two electrons to a bound state
How can electrons form Cooper pairs? Typical Picture

## Slide 7
Bernd Matthias rules：
high symmetry is good, cubic symmetry is the best
high density of electronic states is good
stay away from oxygen
stay away from magnetism
stay away from insulators
stay away from theorists.
Cava’s rule:
发现的超导体的临界温度和发现者经验的指数成反比
Is there any guiding principle for hunting superconductors
Wrong except the 6th rule

## Slide 8
Example: H enriched H3S
Tc decreases with magnetic field
strong isotope shift of Tc in D2S: Tc 185 K for H2S, 90 K for D2S
AP Drozdov, MI Eremets, IA Troyan, Nature 2015
Conventional Wisdom of Raising Tc
To apply high pressure to light elements

## Slide 9
D. Duan et al., Sci. Reports 4, 6968 (2014)
λ ωlog μ* Tc Pressure
2.19 1334.6 K 0.1~0.13 191-204 K 200 GPa
0.13 184 K 250 GPa
0.13 179 K 300 GPa
H3S
Agree with DFT prediction for H3S
Conventional Wisdom of Raising Tc
To apply high pressure to light elements
H enriched H3S: possible 190K superconductor at 200 GPa

## Slide 10
How to Hunt High-Tc Superconductors
  Guiding Principle:
  There is a big chance to find high-Tc superconductors if one can metallize - or other strong chemical bonding electrons

## Slide 11
Common Features of High-Tc Superconducts Revealed
Cuprates still hold the record of highest-Tc at ambient pressure
Cuprate SC
30~160 K
Iron-based SC
30~56 K
MgB2
39 K
H3S and other H-enriched SC
100~280K

## Slide 12
Common Features of High-Tc Superconducts Revealed
Cuprate SC
30~160 K
Iron-based SC
30~56 K
MgB2
39 K
H3S and other H-enriched SC
Quasi-two-dimensional?
Yes
Yes
Yes
No
100~280K

## Slide 13
Common Features of High-Tc Superconducts Revealed
Cuprate SC
30~160 K
Iron-based SC
30~56 K
MgB2
39 K
H3S and other H-enriched SC
Strong antiferromagnetic fluctuations?
Yes
No
No
Yes
100~280K

## Slide 14
Common Features of High-Tc Superconducts Revealed
Cuprate SC
30~160 K
Iron-based SC
30~56 K
MgB2
39 K
H3S and other H-enriched SC
Strong electron-phonon coupling?
probably
probably
Yes
Yes
100~280K

## Slide 15
Common Features of High-Tc Superconducts Revealed
Cuprate SC
30~160 K
Iron-based SC
30~56 K
MgB2
39 K
H3S and other H-enriched SC
Some -bonding electrons become metallized?
Yes
Yes
Yes
Yes
100~280K

## Slide 16
What are -bonding electrons?
-bond: Sideways overlap
-bond: Head-on overlap
strongest covalent bonds
Crystal structure is generally stabilized by -bonds
Metallizing -bonding electrons generally mean melting the lattice

## Slide 17
Why are σ-bonding electrons relevant to high-Tc SC?
Characteristic energy scale of σ-bond is very strong: ~ 3 eV
  the coupling between σ-bonding electrons and phonons is very strong in order to stabilize this bond
  -electrons are difficult to be metallized: this explains why high-Tc SC are so difficult to find
Metallzing σ-electrons reduces the coupling of these electrons, but the residual interaction can still be very large, which serves as a strong glue of Cooper pairs

## Slide 18
Metallizing σ-electrons: Cuprates
Cuprate SC
Cu 3d(x2-y2) and O 2p form a -bond
O 2p
Cu 3d9
Cu 3d10
On-site Coulomb
Repulsion
5-8 eV
-bond
Hole doping lifts the Cu-O -bonds to the Fermi level, leading to high-Tc SC
-bond
Fermi level

## Slide 19
Metallizing σ-electrons: Hole Doping
Cuprate SC
Cu 3d(x2-y2) and O 2p hole form a metallized Zhang-Rice singlet
O 2p
Cu 3d9
Cu 3d10
On-site Coulomb
Repulsion
5-8 eV
-bond
Roles of antiferromagnetic fluctuations
    release the lattice instability induced by doping
    enforce the metallization
Zhang-Rice singlet
Fermi level

## Slide 20
Experimental Evidence of Metallized σ-electrons
Armitage et al., PRL 88, 257001 (2002)
Hole pocket
Electron pocket
Nd2-xCexCuO4
O 2p
Cu 3d9
Cu 3d10
On-site Coulomb
Repulsion
5-8 eV
Zhang-Rice singlet
Fermi level

## Slide 21
Role of Cu-Spin Antiferromagntic Fluctuations
Both the Cu-O σ-bonding electrons and Cu-Cu spins are coupled by the Heisenberg interaction
  Cu-Cu spin antiferromagnetic fluctuations break the bonds and favor the metallization of σ-electrons

## Slide 22
-band is located below the Fermi level, no contribution to conductivity
graphite
Metallizing -electrons: MgB2
-bands
-bands

## Slide 23
Can We Lift -electrons to the Fermi Level?
-bands
-bands
-bands

## Slide 24
Can We Lift -electrons to the Fermi Level?
-bands
MgB2
Mg2+ couples stronger with the 2p -electrons and the 2p -electrons, which lowers the Fermi level of -bands --- effectively lifting the -bands
JM An & WE Pickett, PRL 86, 4366 (2001)

## Slide 25
Can We Lift -electrons to the Fermi Level?
MgB2
Mg2+ couples stronger with the 2p -electrons and the 2p -electrons, which lowers the Fermi level of -bands --- effectively lifting the -bands
Tc = 39 K
J. Nagamatsu et al., Nature 410, 63 (2001)

## Slide 26
N. Bernstein, CS Hellberg, MD Johannes, II Mazin, MJ Mehl, PRB 91, 060511(R) (2015)
H3S
“H3S has a record high Tc due to its covalent bonds driven metallic”
Metallizing σ-electrons: H-enriched Materials

## Slide 27
Theoretical predictions for a number of candidates of high-Tc superconductors

## Slide 28
-bands
LiBC
1. Hole doped LiBC
gap 1.0 ~ 2.5 eV
LiBC: σ-electrons are on the top valence bands
JM An & WE Pickett, PRL 86, 4366 (2001)

## Slide 29
Predicted Tc
Li0.5BC
JM An & WE Pickett, PRL 86, 4366 (2001)
Li0.5BC:
 = 1.5
* = 0.09
Tc = 100 K

## Slide 30
Li deficiency Distorts LiBC
Li0.5BC
AM Fogg et al., JACS 128, 10043 (2006 )

## Slide 31
Can We Dope LiBC without Introducing Li Deficiency?
LiBC
Trilayer LiB2C2
-bands
Gao, Yan, Lu, Xiang, arXiv:1911.12690

## Slide 32
Trilayer LiB2C2
Trilayer LiB2C2 is structurally stable
No imaginary frequency in the spectrum
Gao, Yan, Lu, Xiang, arXiv:1911.12690

## Slide 33
Trilayer LiB2C2
Trilayer LiB2C2 is a Good High-Tc Candidate
Superconducting energy gap as a function of temperature
Obtained by solving Eliasberg equation
Tc ~ 92 K
Gao, Yan, Lu, Xiang, arXiv:1911.12690

## Slide 34
Li3B4C2 : Tc ~ 50 K
M Gao, ZY Lu, T Xiang, PRB 91, 045132 (2015)
Li3B4C2 and Li2B3C: dope holes without introducing lattice distortions
Li2B3C: Tc ~ 55 K
Hole doped LiBC: More suggestions

## Slide 35
2. Materials analog to the cuprates
Cuprate SC
Iron-based SC
There is high chance to find metallized -bonding electrons in materials isostructural and isoelectronic to cuprate superconductors
They may become high-Tc SC by doping
Cu
O
Fe
Se
CuO2 plane
Fe2Se2 layer

## Slide 36
Nd0.8Sr0.2NiO2
Sr2RuO4
Tc ~ 2 K
Superconducting materials isostructural to cuprates
Maeno et al., Nature (1994)
Sr2IrO4
Kim et al, PRL (2012)
Li et al., Nature (2019)
Tc ~ 50 K ?
STM, no transport
Tc ~ 9 - 15 K

## Slide 37
Nd0.8Sr0.2NiO2
Sr2RuO4
weak bonding
weak AFM fluctuation
Are they electronically similar to cuprates?
Sr2IrO4
spin-orbital coupling
AFM fluctuation
surface doping only
3d-4f hybridized
weak AFM fluctuation
weak Ni 3d-O 2p bond

## Slide 38
Can we find a Fe-based analog of the cuprate?
Fe2Se2 layer
CuO2 plane
Zhao, Ma, Lu, Xiang, arXiv:1910.03545
AFeSe2: Fe-based superconducting analogs of the cuprates,
FeSe2 layer

## Slide 39
FeSe2 layer
This kind of material exists: AFeSe2 (A=Tl, K, Rb, Cs)
CuO2 plane
AFeSe2 (A=Tl, K, Rb, Cs)
I-4m2 symmetry Group
TlFeSe2 synthesis
A. Kutoglu, Naturwissenschaften 61, 125 (1974)
G. D. Guseinov et al., Inorg. Mat. 27, 377 (1991)

## Slide 40
Other Structures of AFeSe2
AFeSe2 (A=Tl, K, Rb, Cs)
I-4m2 symmetry Group
KFeSe2, RbFeSe2
Bronger et al., J. Solid State Chem. (1987
C2/c
Quasi-1D antiferromagnetic semiconductor
2-3 B/Fe
C2/m
TlFeSe2: Klepp and Boller, Monatshefte fur Chemie/Chemical Monthly (1979)
CsFeSe2: Stuble and Rohr, Zeitschrift fr anorganische und allgemeine Chemie (2017)
FeSe4 chains
v

## Slide 41
AFeSe2 is similar to the cuprate parent compounds
AFeSe2: charge gap
Tl, K: 22meV
Rb: 56meV
Cs: 98meV
Cuprate: 2 eV
FeSe2 layer
AFeSe2 is an antiferromagnetic insulator
The ground state is Neel ordered

## Slide 42
Antiferromagnetic coupling in AFeSe2
FeSe2 layer
comparable to cuprates
meV/S2
3.6 /Fe

## Slide 43
Spin density
Fe-Se: Strong covalent hybridized
Fe-Fe: No direct interaction
Magnetic interaction between Fe moments arises from Se-bridged AFM superexchange
AFeSe2: Charge and Spin Density Distribution
FeSe2 layer
Charge density

## Slide 44
Summary
Metallizing strong bonding electrons provides a universal route to high-Tc superconductivity
LiB2C2, Li3B4C2, Li2B3C, and doped AFeSe2 (A=Tl,K,Rb,Cs) are good candidates of high-Tc SC
Zhongyi Lu
Renmin Univ China
Miao Gao
Ningbo University
Fengjie Ma Xinlei Zhao
Beijing Normal University
Xunwang Yan
Qufu Normal Univ

## Slide 45
Thank you for your attention!

## Slide 46
1, 2, 3 electron-type FS 4 hole-type FS
No Fermi-surface nesting
1
2
3
4
TlFeSe2 : Band Structure in the Nonmagnetic Phase

## Slide 47
Boron doped diamond
Tc = 4 K 2.8% B
E. A. Ekimov et al. , Nature (London) 428, 542 (2004).
Low density of states at Fermi level

## Slide 48
H enriched H3S: possible 190K superconductor at 200 GPa
resistivity is 50 times lower than the copper resistivity
Tc decreases with magnetic field
strong isotope shift of Tc in D2S: Tc 185 K for H2S, 90 K for D2S
AP Drozdov, MI Eremets, IA Troyan, Nature 2015
Conventional Wisdom of Raising Tc
To apply high pressure to light elements

## Slide 49
D. Duan et al., Sci. Reports 4, 6968 (2014)
λ ωlog μ* Tc Pressure
2.19 1334.6 K 0.1~0.13 191-204 K 200 GPa
0.13 184 K 250 GPa
0.13 179 K 300 GPa
H3S
Agree with DFT prediction for H3S
Conventional Wisdom of Raising Tc
To apply high pressure to light elements
H enriched H3S: possible 190K superconductor at 200 GPa

## Slide 50
What is a superconductor?
Perfect conductor
Perfect diamagnet
Resistivity vanishes in the superconducting state
Messiner effect
Anderson-Higgs Mechanism

## Slide 51
Bardeen Cooper Schrieffer
1957
How to become superconducting
Electrons form Cooper pairs
via electron-phonon or other interactions
Cooper pairs condense
to form phase coherence
Superconductivity